## Slide 1
Three Key Classification Criteria
Permeance – resistance to migration of moisture
Impact/puncture resistance
Tensile Strength
Construction Underlayment Film
Construction Underlayment/Vapor barrier wrap
Provides a barrier to moisture migration from the ground into the building
Prevents issues such as mold growth, concrete degradation, and potential damage to building materials
Three Classes of Vapor Barrier Underlayment Film
Class A, Class B, and Class C
Same barrier/permeance performance requirement of 0.1 perms for Class A – Class C
Classes differentiated based upon puncture and tensile strength
Market Insights
Heavy gauge structures varying in thickness from 6 – 20+mil
Solution utilized depends on building requirements, geography, and local building codes
Key Performance Property | Class A | Class B | Class C
Water Vapor Permeance | 0.1 perms | 0.1 perms | 0.1 perms
Tensile Strength | 45.0 lbf/in. | 30.0 lbf/in. | 13.6 lbf/in.
Puncture Resistance Dart Impact | 2.200 grams | 1.700 grams | 475 grams

## Slide 2
Industry Codes & Standards
International Building Code
International Residential Code
ASTM International
American Concrete Institute
ASTM E1745 - Standard Specification for Plastic Water Vapor Retarders Used in Contact with Soil or Granular Fill under Concrete Slabs
  Class A, B, or C
  All under slab structures are Class I materials
ASTM E154 - Standard Test Methods for Water Vapor Retarders Used in Contact with Earth Under Concrete Slabs, on Walls, or as Ground Cover
Vapor retarder Class I, II, or III based upon building codes
Section 1907 – Slabs on Ground
R506.2.3 Vapor retarder must be a minimum of 10 mil
State and local codes leverage framework established by these industry organizations.
ACI 302.1R-15 - GUIDE TO CONCRETE FLOOR AND SLAB CONSTRUCTION

## Slide 3
Key Performance Property | ASTM Method | Units | ASTM E1745 Class A | 10A | 15A | 20A
Water Vapor Permeance 23°C, 100% RH | F1249 | perms | 0.1 | 0.017 | 0.008 | 0.004
Tensile Strength | D882 | lbf./in | 45 | 50 | 80 | 90
Puncture Resistance | D1709 | grams | 2,200 | >3,300 | >3,000 | >3,300
Construction Underlayment
ASTM E1745 Class A Product Performance

## Slide 4
Permeance
Chart: Permeance ASTM F1249
| ASTM E1745 Class A | 10A | 15A | 20A
Permeance | 0.1 | 0.017 | 0.008 | 0.004
Permeance exceeds Class A requirements
10A, 15A, and 20A are below 0.1 perms
15A and 20A are below 0.01 perms
Performance Property Summary

## Slide 5
Tensile Strength
Chart: Tensile Strength ASTM 882
| ASTM E1745 Class A | 10A | 15A | 20A
Tensile | 45 | 50 | 80 | 90
Tensile Strength, lbf./in
MD/TD
Tensile Strength exceeds Class A requirements
10A, 15A, and 20A are above minimum of 45 lfb./in in MD and TD direction
Performance Property Summary

## Slide 6
Puncture Resistance
Chart: Dart ASTM D1709
| ASTM E1745 Class A | 10A | 15A | 20A
Dart | 2200 | 3300 | 3000 | 3300
Dart exceeds Class A requirements
10A, 15A, and 20A are above 2,200 grams
Performance Property Summary
ASTM E1745
Class A
10A
15A
20A